## Slide 1
Figure 1. XRD analysis of iron ore, slime and mill scale

## Slide 2
(a) Iron ore fine
(b) Mill scale fine
(c) Slime fine
Figure 2. Surface morphology of different fines under SEM microscope

## Slide 3
Figure 3. Thermo-gravimetric analysis of several raw materials

## Slide 4
Chart: Basicity (CaO/SiO2) / ratio
| 0 | 0.30000000000000032 | 0.5 | 0.8
CCS | 231 | 409 | 412 | 432
RDI | 86.76 | 19.18 | 26.749 | 59.3814
Figure 4. Effect of Basicity on CCS and RDI of indurated fluxed pellet
Induration temperature: 1275 °C

## Slide 5
Chart: Slime addition/ wt%
| 0 | 5 | 10 | 15
CCS | 328.142 | 288.77 | 255.2313 | 249.6173
AP | 23.0249 | 23.4368 | 23.7696 | 24.0607
Figure 5. Effect of increasing addition of iron ore slime on the CCS and Apparent Porosity of mill scale containing acidic hematite pellet
Mill scale content: 15 wt%

## Slide 6
Figure 6. Optical microstructure of mill scale added acidic pellets with and without addition of iron ore slime

## Slide 7
Figure 7. XRD pattern of mill scale added acidic pellet and with and without the addition of iron ore slime

## Slide 8
Chart: Iron ore slime addition/ wt%
| 0 | 5 | 10 | 15
RDI | 25 | 44.84 | 48.07 | 49.22
Figure 8. Effect of iron ore slime addition on RDI of mill scale added hematite pellet
Mill scale: 15 wt%

## Slide 9
Chart: Iron ore slime addition/ wt%
| 0 | 5 | 10 | 15
1275 | 411 | 410 | 442 | 447.22
1175 | 271.06 | 279 | 287 | 303
1200 | 322.17 | 313 | 362 | 366
Mill Scale: 15wt%
Basicity : 0.3
Figure 9. Effect of iron ore slime addition on the CCS of mill scale added basic hematite pellet

## Slide 10
Chart: Iron ore slime addition, wt%
| 0 | 5 | 10 | 15
AP | 19.9679 | 18.8312 | 17.9398 | 17.9224
Mill Scale: 15 wt%
Basicity : 0.3
Induration temperature: 1275 °C
Figure 10. Effect of iron ore slime addition on the AP of mill scale added basic hematite pellet

## Slide 11
(a) 15 wt % mill scale added pellet without slime (Indurated at 1275°C) (b) 15 wt% mill scale added pellet with 15% slime (Indurated at 1275°C)
Figure 11. XRD of mill scale added basic pellet (0.3 basicity) with and without the addition of iron ore slime

## Slide 12
15 wt% mill scale added pellet with 15 wt% slime (Indurated at 1275°C)
15 wt% mill scale added pellet without slime (Indurated at 1275°C)
1:Hematite, 2: pore, 3: slag, 4: Magnesio ferrite
Figure 12. Optical microstructure of mill scale added basic pellet (0.3 basicity) with and without the addition of iron ore slime

## Slide 13
Chart: Iron ore slime addition/ wt%
| 0 | 5 | 10 | 15
RDI | 6.4 | 11.22 | 10.39 | 12.66
Mill Scale: 15 wt%
Basicity : 0.3
Induration temperature: 1275 °C
Figure 13. Effect of iron ore slime addition on RDI of mill scale added basic hematite pellet