Vojnosanit Pregl 2014; 71(7): 673–678.
VOJNOSANITETSKI PREGLED
Strana 673
Volumen 63, Broj 1
VOJNOSANITETSKI PREGLED
Strana 1

[image: image1.wmf]GENERAL REVIEW 

UDC: 615.46::[616.6-08:618.1-08

DOI:10.2298/VSP1407673I

Experimental and clinical use of meshes in urogynecology

Eksperimentalna i klinička upotreba sintetskih hirurških mrežica u uroginekologiji 

Ivan M. Ignjatović, Milan B. Potić

Clinic of Urology, Clinical Center Niš, Niš, Serbia

Key words:


urinary incontinence, stress; pelvic organ prolapse; surgical mesh; treatment outcome.


Ključne reči:

inkontinencija, urinarna, stres; karlični organi, prolaps; hirurška mrežica; lečenje, ishod.

Introduction

The most common problems in urogynecology, stress urinary incontinence (SUI) and pelvic organ prolapse (POP) are, in other words, problems of pelvic organ support. Extended demand for support in pelvic reconstructive surgery has led to the development of both biomaterials and synthetic grafts. The ideal biomaterial should be physically and chemically inert, mechanically strong, noncarcinogenic, easily fabricated and stabilized, and should induce minimal inflammatory reaction 1.

Experimental studies and mesh behavior

Several studies have analyzed biomaterials derived from dermal, pericardial, dural, and other anatomical sources, and have emphasized their non-uniform graft behavior, variable preparation, and unpredictable quality 2. Synthetic grafts clearly demonstrated superior durability and long-term success over biomaterials for pelvic floor repair 3.

The most widely accepted method of testing synthetic grafts is through experimental animal studies. In analyzing the literature, it is obvious that rats are the most commonly accepted experimental model. Several study groups have set the standard for methods as well as tissue analysis and tensile strength in experimental studies 4, 5. Primary repair of full-thickness abdominal wall defect, with respect to the peritoneum, seems like a logical choice. Monofilament polypropylenes were theoretically and practically the first choice for testing, considering the assumption that multifilaments are prone to infection 4. There is consensus that an average of 90-µm pore size provides the best mechanical anchorage, with peak in-growth reached at around 400–500 µm 1, 2. Larger pores limit the deposition of collagen to the perifilament region, with central parts being deposited with fat. A solid product, as well as one with smaller pores (< 50 µm), can lead to complete encapsulation or induce an intensive inflammatory reaction. In addition, the intensity of an inflammatory reaction is determined by the amount of synthetic material, therefore suggesting the use of lighter materials 1, 4 6.
It is presumed that multifilaments with interfilamentous spaces smaller than 10 µm are prone to infection, bearing in mind that macrophages are 15 µm in diameter, and bacteria 1–2 µm. Multifilaments were theoretically supposed to have better elasticity, but the same results are achieved with low weight monofilaments 4, 5. After an initial polypropylene testing, some advances in biocompatibility were to be revealed experimentally on a polypropylene-coated field. Collagen-coated and titanium-coated grafts were to express a less intensive inflammatory reaction, with the same results, on a field of collagen deposition; however, they failed 6. Arginine administration was also evaluated in experimental models for improved mesh integration, but the experimental data are inconclusive 7. Some rather interesting data were revealed on initial experimental analysis of semi-reabsorbable (polypropylene-polyglactin) grafts 6. Later studies determined that the semi-reabsorbable combination proved to be a stable scaffold for collagen deposition, leaving less foreign material after polyglactin reabsorption, with no consequences on tensile strength 5. Experimental studies have revealed a totally new perspective on the mechanical analysis of incorporated grafts. Tensiometric studies of native graft samples have indicated significant differences in strength among tested samples. When colonized by cells and incorporated with native tissue, explanted samples provided comparable tensiometric strength, regardless of the material used 5. Some studies even reported that stronger tensiometric results were achieved with monofilaments than with multifilaments 4.

Experimental studies have suggested a high modality and uniform quality of synthetic meshes, with a rather steady retraction rate of about 20% 1, 4, 5. Graft retraction seems to correlate with stiffness parameters in the elastic domain of graft deformation 5. Retraction rates, when summarized, highlight the well-known postulate of tension-free surgery.

Consensus on a cascade Worman’s effect is almost absolute. Protein covering of the graft and inflammatory reaction within the first three weeks are the initial steps of foreign body reaction 1. The reparation process, regardless of the experimental animal model, is characterized by collagen deposition and final stabilization within six weeks 4, 5.

One study even analyzed cell oxidative stress levels in relation to the mesh material used 5. Conclusions definitely confirmed a positive correlation between cell oxidative stress and the amount of implanted synthetic material. In summary, rat studies have shown good biocompatibility, respectable tensile strength, and fewer complications.

In several studies, rabbits were chosen as an experimental model, but they showed no difference in graft behavior 8. Pigs are less common, considering that large animals are not as easy to manipulate, and the experimental samples are smaller. The highest level of retraction reported in an experimental study on pigs is 30% 9. However, this result should be considered cautiously, as retraction was measured with millimeter paper alone. One of the interesting, but rare, experimental studies conducted on very large animals included horses 10. Fifteen horses were treated with polypropylene meshes for large abdominal hernias and the results were exceptional, except for one fatality.

In summary, future perspectives seem to favor semi-reabsorbable, low-weight monofilament meshes, with totally inert synthetic grafts being the ultimate theoretic goal.

Mesh in the treatment of stress urinary incontinence

Stress urinary incontinence is a highly prevalent (41%) problem; 72% of patients have moderate to severe symptoms, with only 25% seeking professional help 11. There is a prognosis that requirements for surgery will increase up to 45% in the future, due to less tolerance of SUI symptoms by patients and the normal aging of female population expected in western countries 12. Synthetic materials have been generally used in the treatment of SUI after wide acceptance of the Petros and Ulmsten theory of continence 13. The sling was moved from the bladder neck to the midurethral position and placed in a tension-free manner. The role of the sling is support of the urethra, instead of previous tension sutures placed on the bladder neck or a fascial sling placed on the same position 14, 15.

The sling is placed retropubically, transobturatory, or as a mini (single incision) sling. Tension-free placement has contributed to their non-obstructive behavior, low incidence of urinary retention, no exaggeration of prolapse, and decreased deterioration of the posterior compartment 16, 17. Postoperative sexual dysfunction is infrequent, due to an unchanged vaginal axis, which is the most frequently recognized flaw of the Burch operation 18, 19. Retropubic placement of the sling requires cystoscopy as a mandatory part of the procedure, and sling placement was limited in very obese patients and in patients with previous pelvic surgery and suspicious intestinal adhesions. Transobturatory placement performed “inside out” or “outside in” (both ways are almost equal, with “inside out” being slightly superior) 20, 21 became an acceptable alternative that does not require cystoscopy and does not affect the abdominal cavity. Mini slings are the least invasive, placed in a U position or horizontally. There were high expectations and hopes because of the convenient pain profile, but the results were not as encouraging, and their use is performed with caution 22–24. There are also self-tailored modifications or industrial modifications of the sling, which are applied with similar or equal success rates 25, 26.
However, no one way of sling placement is absolutely complication free 27, 28. This is especially important to keep in mind, because the surgery is performed with the aim of improving quality of life, and dangerous reported complications, such as bowel perforation and serious bleeding (the majority after retropubic sling surgery), can compromise the procedure seriously.

Success rate (effectiveness) is measured subjectively (interviews, different questionnaires), objectively (e.g. 24-hour pad test, stress test), or as a combined evaluation after surgery. Subjectively evaluated success is always higher than objectively measured one, and varies between 85.7% and 91.6%. The number of satisfied females with significant improvement is higher than the number of completely dry patients 29.

Unfortunately, dryness is not the only outcome of the surgery. Complication rates should not be neglected, but they are usually underreported. The reported complication rate is 4.3–75.1% for retropubic and 10.5–31.3% for transobturatory midurethral slings 30. The most important predictive factors for sling failure are documented intrinsic sphincter deficiency (ISD) and fixed urethra. It is assumed, in other words, that in patients with a fixed urethra, the main problem is low resistance at the level of the bladder neck, and not urethral support, so the support improvement achieved by the sling is less likely to be curative. Fortunately, the results of tension-free tape (TVT) and adjustable slings in these patients are only a little inferior, or equal, to the results of TVT (66% and 85% cured patients, respectively) 30, 31. There is a documented follow-up of patients with suprapubic TVT–11.5 years and transobturator tabe (TOT) – 6.5 years, without significant differences between the procedures. Both of these procedures have a stable, long-term success rate (77% and 83%, respectively) 32, 33. The difference was not spectacular compared with the Burch Tangho operation (70% dry patients) 34.
Recurrent SUI is not an uncommon problem after tension-free procedures. The success rate is lower than after primary treatment (63.5% dry), but it is still acceptable. There is scarce evidence of favorable types of slings for the “redo” surgery, but the retropubic sling seems to be more effective than the transobturatory sling 35, 36.
Postoperative voiding dysfunction and urinary retention after sling procedures are underreported. Frequency of urinary retention (1.8–10%) is highest in patients with the retropubic sling, but it is not absent with the transobturatory or single-incision sling. It is usually temporary, and intermittent catheterization or catheter removal several days later solves the problem. Long-term retention (15 days) usually requires pulling down the sling or a sling section, or removal of the sling. In the majority of cases, it does not result in the recurrence of SUI 37–41.

There was a confusing terminology in previous years regarding the complications-sling exposition and erosion. It is accepted now that sling exposition describes a visible sling in the vagina, uncovered by the vaginal epithelium. Sling erosion is a penetration of the sling into the adjacent viscera. The more frequent surgical complications of the sling is exposition (13%) 41, 42. Sling exposition is usually expressed as vaginal discharge, pain during intercourse, or sexual discomfort. Sometimes it occurs up to ten years after the surgery 42, 44. Sling erosion is the consequence of such conditions as migration in the urinary bladder or urethra, or abscess formation. In extreme cases, consequent vesicovaginal or uterovaginal fistulas are possible 45, 46. Possible explanations for sling exposition are insufficient surgical skill, structure of the sling material, or susceptibility of the hammock to the sling 42. Sexual function could be improved (29.5% and 32.5% for TVT and TOT, respectively), deteriorated (17.3% and 12.5%), or unchanged after the sling procedures 47. The vast majority of patients will have improvement in their sexual life, but statements about postoperative sexual function must be included in the informed consent before the surgery 47–49.

Overactive bladder symptoms and mixed urinary incontinence are not contraindications for the sling. Postoperative urgency could start before the surgery and remain after the surgery, or appear as a phenomenon de novo 50, 51. Preoperative urgency is more frequent in patients; mixed urinary incontinence, age, nocturia, maximum cystometric capacity, and choice of sling procedure influence detrusor overactivity and urge urinary incontinence 52. In the majority of cases, postoperative urgency is sensory and can be controlled with anticholinergics. If urgency persists, removal of the sling is mandatory 53.
Mesh in the treatment of pelvic organ prolapse

Pelvic organ prolapse is a frequent disease among the aging female population. Almost 11% of the female population up to the age of 80 will require some type of surgical correction of POP 54. Generally, correction of POP is performed with native tissue (NAT repair), mesh adjunct (pure synthetic material, resorbable or not), or rarely, graft (biological material), is used to repair the pelvic floor. Corrections are usually undertaken because of the anatomical disorder (vaginal bulge) and/or coexisting symptoms of prolapse included in symptom/bothersome symptom questionnaires. Vaginal bulge is the most prominent symptom; others include pelvic pressure, associated incontinence or urinary retention and bowel emptying problems, and sexual dysfunction.

Several major influences on POP surgery have been recognized: extensive reports that some degree of prolapse is not obviously symptomatic, changing criteria for performing surgery, and differences in the evaluation of surgery outcome.
Normal anatomic prolapse variations were well recognized in a study of routine clinical examinations of asymptomatic females, and it was confirmed that POP stage I is present in 38%, and stage II in 35% of patients. If it is evaluated as a result of surgery, more than 75% will not meet the criteria for ideal, and 40% for satisfactory outcome 55. To mitigate a tendency to surgically “overcorrect” the anatomy of asymptomatic females, the evaluation criteria have changed. Acceptable results of successful repair are absent prolapse beyond the hymen, no symptoms, and no need for additional treatment 56. Therefore, the main advantage of the polypropylene mesh superior anatomical restoration of the female genitalia was lost. In anterior vaginal repair, the efficiency of mesh surgery was confirmed to be superior to that of non-mesh surgery, which has a failure rate of 29% 57. Ten randomized control studies showed that synthetic absorbable mesh has the highest failure rate (23%), followed by biological graft (18%) and non-absorbable synthetic mesh (5%) 57. Safety was highest in cases with absorbable mesh (exposure rate, 0.6%), followed by biological grafts (6%) and synthetic non-absorbable mesh (10%) 57. Posterior repair, with or without mesh, is significantly less frequently reported, and there is no confirmed evidence of a clear superiority of the special method of posterior compartment repair 58. Clinical experience suggests that mesh will surely keep its place in strict indications (mesh compared to non-mesh surgery: recurrent prolapse/success rate, 90.4% versus 54.8%, respectively; paravaginal defect, 97.6% versus 65.6%; badly damaged pelvic floor, 64% versus 22.9% 59, 60. Symptoms after mesh correction are based on clinical studies, and use of the mesh was not proved in lower grade prolapse 61. In other words, restoring anatomy does not mean restoring symptoms at the same time.

Apical defect, although less frequently discussed, is a normal prerequisite for the success of POP surgery. It can be performed with adequate success using a variety of surgical options: vaginal sacrospinous support with mesh (tailored or modified), or colposacral fixation performed by robotics, laparoscopy, or open surgery 62, 63. Safety of the mesh surgery is lower, according to reported complications, some of them dangerous or life threatening 64, 65.

Sexual dysfunction increases constantly with age. The frequency of sexual dysfunction is up to 50%, and it has a multifactorial origin 66. Surgeries of any type, as well as concomitant gynecological pathology, could deteriorate sexual function without reliable data to address the source of sexual dysfunction to the mesh directly 67. However, the Food and Drug Administration (FDA) has recently issued warnings regarding increased complications of mesh surgery and the exaggerated justification for its use in clinical settings 68, 69. Almost no one could ignore these statements 68.

Finally, all aspects of POP must be evaluated carefully: anatomy, symptoms, quality of life, late complications, and possible repeated surgeries 69. We have to create a treatment design to meet the criteria of the patients more comprehensively, with native tissue repair whenever it is possible, and with mesh only when it is absolutely necessary.

Conclusion

Synthetic materials have been developed constantly during previous decades, but they have not achieved the standards of ideal foreign material. Their biologic behavior is still unknown, especially after long-term follow-up. Improvements in the treatment of stress urinary incontinence are remarkable, and polypropylene slings have met the criteria for the gold standard of treatment, both for the suprapubic and transobturatory routes of application. It is not the same for mini slings. Meshes in pelvic organ prolapse surgery are superior for the correction of anatomy, but the overall benefit of their use is not remarkable, and complications are more frequent. It is certain that recent experiences will substantially diminish the use of mesh in pelvic organ prolapse surgery, as the restoration of anatomy is not a single goal of surgery. However, its use will be kept for selected patients. Improvement of our knowledge, both fundamental and clinical, is necessary for superior pelvic organ prolapse repair.

Acknowledgement 

This work was supported by the Serbian Ministry of Education, Science and Technological Development, grant No. 175092.

REFERENCES

Deprest J, Zheng F, Konstantinovic M, Spelzini F, Claerhout F, Steensma A, et al. The biology behind fascial defects and the use of implants in pelvic organ prolapse repair. Int Urogynecol J Pelvic Floor Dysfunct 2006; 17 Suppl 1: S16−25. 

1. Davila GW, Drutz H, Deprest J. Clinical implications of the biology of grafts: conclusions of the 2005 IUGA grafts roundtable. Int Urogynecol J Pelvic Floor Dysfunct 2006; 17: 51−5.

Feifer A, Corcos J. The use of synthetic sub-urethral slings in the treatment of female stress urinary incontinence. Int Urogynecol J Pelvic Floor Dysfunct 2007; 18(9): 1087−95.

2. Konstantinovic ML, Pille E, Malinowska M, Verbeken E, De Ridder D, Deprest J. Tensile strength and host response towards different polypropylene implant materials used for augmentation of fascial repair in a rat model. Int Urogynecol J Pelvic Floor Dysfunct 2007; 18(6): 619−26.

3. Potic M, Ignjatovic I, Savic V, Djekic P, Radenkovic G. Mechanical properties and tissue reinforcement of polypropylene grafts used for pelvic floor repair: an experimental study. Hernia 2011; 15(6): 685−90.

Pereira-Lucena CG, Artigiani-Neto R, Lopes-Filho GJ, Frazao CVG, Goldenberg A, Matos D, et al. Experimental study comparing meshes made of polypropylene, polypropylene + polyglactin and polypropylene + titanium: inflammatory cytokines, histological changes and morphometric analysis of collagen. Hernia 2010; 14(3): 299−304.

Arbos MA, Ferrando JM, Quiles MT, Vidal J, Lopez-Cano M, Gil J, et al. Improved surgical mesh integration into the rat abdominal wall with arginine administration. Biomaterials 2007; 27: 758−68.

Zhang K, Han JS, Yao Y, Yang J, Qiao J. Local reaction to the different meshes at the vesicovaginal space in rabbit model. Int Urol J 2012; 23(5): 605−11.

4. Cobb WS, Burns JM, Peindl RD, Carbonell AM, Matthews BD, Kercher KW, et al. Textile Analysis of Heavy Weight, Mid-Weight, and Light Weight Polypropylene Mesh in a Porcine Ventral Hernia Model. J Surg Ress 2006; 136(1): 1−7. 

Vilar JM, Doreste F, Spinella G, Valentini S. Double-Layer Mesh Hernioplasty for Repair of Incisional Hernias in 15 Horses. J Equi Vet Sci 2009; 29(3): 172−6. 

5. Minassian VA, Yan X, Lichtenfeld MJ, Sun H, Stewart WF. The iceberg of health care utilization in women with urinary incontinence. Int Urogynecol J 2012; 23(8): 1087−93.

6. Novara G, Ficarra V, Boscolo-Berto R, Secco S, Cavalleri S, Artibani W. Tension-free midurethral slings in the treatment of female stress urinary incontinence: a systematic review and meta-analysis of randomized controlled trials of effectiveness. Eur Urol 2007; 52(3): 663−78. 

7. Petros PE, Ulmsten UI. An integral theory of female urinary incontinence. Experimental and clinical considerations. Acta Obstet Gynecol Scand Suppl 1990; 153: 7−31. 

Papa PP New ambulatory surgical methods using an anatomical classification of urinary dysfunction improve stress, urge and abnormal emptying. Int Urogynecol J Pelvic Floor Dysfunct 1997; 8(5): 270−7. 

Ulmsten U, Henriksson L, Johnson P, Varhos G. An ambulatory surgical procedure under local anesthesia for treatment of female urinary incontinence. Int Urogynecol J 1996; 7(2): 81−6, discussion 85−6.

8. Ward KL, Hilton P. Tension-free vaginal tape versus colposuspension for primary urodynamic stress incontinence: 5-year follow up. BJOG 2008; 115(2): 226−33.

9. Moore C, Paraiso MF. Voiding dysfunction after the tension-free vaginal tape procedure. Curr Urol Rep 2005; 6(5): 356−9. 

Klutke C, Siegel S, Carlin B, Paszkiewicz E, Kirkemo A, Klutke J. Urinary retention after tension-free vaginal tape procedure: incidence and treatment. Urology 2001; 58(5): 697−701. 

10. Madhuvrata P, Ford J, Merrick K, Boachie C, Abdel-Fattah M. Voiding dysfunction following suburethral tape. J Obstet Gynaecol 2011; 31(5): 424−8.

Latthe PM, Singh P, Foon R, Toozs-Hobson P. Two routes of transobturator tape procedures in stress urinary incontinence: a meta-analysis with direct and indirect comparison of randomized trials. BJU Int 2010; 106(1): 68−76. 

Madhuvrata P, Riad M, Ammembal MK, Agur W, Abdel-Fattah M. Systematic review and meta-analysis of "inside-out", versus "outside-in" transobturator tapes in management of stress urinary incontinence in women.. Eur J Obstet Gynecol Reprod Biol 2012; 162(1): 1−10.

Mostafa A, Agur W, Abdel-All M, Guerrero K, Lim C, Allam M, et al. A multicentre prospective randomised study of single-incision mini-sling (Ajust®) versus tension-free vaginal tape-obturator (TVT-O™) in the management of female stress urinary incontinence: pain profile and short-term outcomes. Eur J Obstet Gynecol Reprod Biol 2012; 165(1): 115−21. 

11. Walsh CA. TVT-Secur mini-sling for stress urinary incontinence: a review of outcomes at 12 months. BJU Int 2011; 108(5): 652−7. 

12. Cornu J, Lizée D, Sèbe P, Peyrat L, Ciofu C, Cussenot O, et al. TVT SECUR single-incision sling after 5 years of follow-up: the promises made and the promises broken. Eur Urol 2012; 62(4): 737−8. 

13. Chen X, Tong X, Jiang M, Li H, Qiu J, Shao L, et al. A modified inexpensive transobturator vaginal tape inside-out procedure versus tension-free vaginal tape for the treatment of SUI: a prospective comparative study. Arch Gynecol Obstet 2011; 284(6): 1461−6.

14. Ignjatovic I, Vuckovic M, Srzentic Z. Transobturatory tension-free composite sling for urethral support in patients with stress urinary incontinence: favorable experience after 1 year follow up. Int J Urol 2006; 13(6): 728−32. 

15. Ayoub N, Chartier-Kastler E, Robain G, Mozer P, Bitker MO, Richard F. Functional consequences and complications of surgery for female stress urinary incontinence. Prog Urol 2004; 14(3): 360−73. 

16. David-Montefiore E, Frobert J, Grisard-Anaf M, Lienhart J, Bonnet K, Poncelet C, et al. Peri-operative complications and pain after the suburethral sling procedure for urinary stress incontinence: a French prospective randomised multicentre study comparing the retropubic and transobturator routes. Eur Urol 2006; 49(1): 133−8. 

Okulu E, Kayigil O, Aldemir M, Onen E. Use of three types of synthetic mesh material in sling surgery: A prospective randomized clinical trial evaluating effectiveness and complications. Scand J Urol 2012; (In press)

Sergent F, Popovic I, Sentilhes L, Verspyck E, Lemoine JP, Marpeau L. Le TVT (tension-free vaginal tape) a-t-il une place dans le traitement de l’insuffisance sphinctérienne . J Gynecol Obstet Biol Reprod (Paris) 2004; 33(3): 210−20. 

17. Giberti C, Gallo F, Cortese P, Schenone M. The suburethral tension adjustable sling (REMEEX system) in the treatment of female urinary incontinence due to 'true' intrinsic sphincter deficiency: results after 5 years of mean follow-up. BJU Int 2011;108(7): 1140−4. 

18. Fong ED, Nitti VW. Review article: Mid-urethral synthetic slings for female stress urinary incontinence. BJU Int 2010; 106(5): 596−608. 

Heinonen P, Ala-Nissilä S, Räty R, Laurikainen E, Kiilholma P. Objective cure rates and patient satisfaction after the transobturator tape procedure during 6.5-year follow-up. J Minim Invasive Gynecol 2013; 20(1): 73−8. 

19. Lapitan MC, Cody JD. Open retropubiccolposuspension for urinary incontinence in women. Cochrane Database Syst Rev 2012; 6: CD002912.

20. Verbrugghe A, de Ridder D, Van der Aa F. A repeat mid-urethral sling as valuable treatment for persistent or recurrent stress urinary incontinence. Int Urogynecol J 2013; 24(6): 999−1004.

21. Hashim H, Terry T. Management of recurrent stress urinary incontinence and urinary retention following midurethral sling insertion in women. Ann R Coll Surg Engl 2012; 94(7): 517−22. 

Kim JH, Shin SH, Oh MM Park JY, Lee JG, Bae JH. Factors affecting transient urinary retention after transobturator tape mid-urethral sling surgery for female patients with stress urinary incontinence: a single center experience. Eur J Obstet Gynecol Reprod Biol 2013; 168(1): 107−11.

22. Minassian VA, Al-Badr A, Drutz HP, Lovatsis D. Tension-free vaginal tape, Burch, and slings: are there predictors for early postoperative voiding dysfunction? Int Urogynecol J Pelvic Floor Dysfunct 2004; 15(3): 183−7. 

23. Sokol AI, Jelovsek JE, Walters MD, Paraiso MF, Barber MD. Incidence and predictors of prolonged urinary retention after TVT with and without concurrent prolapse surgery. Am J Obstet Gynecol 2005; 192(5): 1537−43. 

24. Reich A, Kohorst F, Kreienberg R, Flock F. Voiding dysfunction after the tension-free vaginal tape procedure. Gynecol Obstet Invest 2011; 72(2): 79−84. 

Glavind K, Glavind E. Treatment of prolonged voiding dysfunction after tension-free vaginal tape procedure. Acta Obstet Gynecol Scand 2007; 86(3): 357−60. 

25. Domingo S, Alamá P, Ruiz N, Perales A, Pellicer A. Diagnosis, management and prognosis of vaginal erosion after transobturator suburethral tape procedure using a nonwoven thermally bonded polypropylene mesh. J Urol 2005; 173(5): 1627−30. 

26. Robert M, Murphy M, Birch C, Swaby C, Ross S. Five cases of tape erosion after transobturator surgery for urinary incontinence. Obstet Gynecol 2006; 107(2 Pt 2): 472−4. 

27. Khanuengkitkong S, Lo TS, Dass AK. Delayed vaginal and urethral mesh exposure: 10 years after TVT surgery. Int Urogynecol J 2013; 24(3): 519−21.

Mustafa M, Wadie BS. Bladder erosion of tension-free vaginal tape presented as vesical stone; management and review of literature. Int Urol Nephrol 2007; 39(2): 453−5. 

28. Estevez JP, Cosson M, Boukerrou M. An uncommon case of urethrovaginal fistula resulting from tension-free vaginal tape. Int Urogynecol J 2010; 21(7): 889−91. 

Sentilhes L, Berthier A, Loisel C, Descamps P, Marpeau L, Grise P. Female sexual function following surgery for stress urinary incontinence: tension-free vaginal versus transobturator tape procedure. Int Urogynecol J Pelvic Floor Dysfunct 2009; 20(4): 393−99. 

29. Pace G, Vicentini C. Female sexual function evaluation of the tension-free vaginal tape (TVT) and transobturator suburethral tape (TOT) incontinence surgery: results of a prospective study. J Sex Med 2008; 5(2): 387−93. 

30. King AB, Wolters JP, Klausner AP, Rapp DE. Vaginal symptoms and sexual function after tension-free vaginal tape-obturator placement: minimum 12-month follow-up. Urology 2013; 81(1): 50−4. 

31. Athanasiou S, Grigoriadis T, Giannoulis G, Protopapas A, Antsaklis A. Midurethral slings for women with urodynamic mixed incontinence: what to expect. Int Urogynecol J 2013; 24(3): 393−9.

32. Botros SM, Miller JR, Goldberg RP, Gandhi S, Akl M, Beaumont JL, et al. Detrusor overactivity and urge urinary incontinence following trans obturator versus midurethral slings. Neurourol Urodyn 2007; 26(1): 42−5. 

Botros SM, Abramov Y, Goldberg RP, Beaumont JL, Gandhi S, Miller JR, et al. Detrusor overactivity and urge urinary incontinence [corrected] following midurethral versus bladder sling procedures. Am J Obstet Gynecol 2005; 193(6): 2144−8. 

33. Segal JL, Vassallo B, Kleeman S, Silva AW, Karram MM. Prevalence of persistent and de novo overactive bladder symptoms after the tension-free vaginal tape. Obstet Gynecol 2004; 104(6): 1263−9. 

Fialkow MF, Newton KM, Lentz GM, Weiss NS. Lifetime risk of surgicalmanagement for pelvic organ prolapse or urinary incontinence. Int Urogynecol J Pelvic Floor Dysfunct 2008; 19(3): 437−40.

Swift S, Woodman P, Boyle AO, Kahn M, Valley M, Bland D, et al. Pelvic Organ Support Study (POSST): the distribution, clinical definition, and epidemiologic condition of pelvic organ support defects. Am J Obstet Gynecol 2005; 192(3): 795−806. 

34. Jacquetin B. Traditional native tissue vs mesh-augmented pelvic organ prolapse repairs: providing an accurate interpretation of current literature. Comment. Int Urogynecol J 2013; 24(1): 181−82.

35. Jia X, Glazener C, Mowatt G, MacLennan G, Bain C, Fraser C, et al. Efficacy and safety of using mesh or grafts in surgery for anterior and/or posterior vaginal wall prolapse: systematic review and meta-analysis. BJOG 2008; 115(11): 1350−61. 

36. Ostergard DR. Evidence-based medicine for polypropylene mesh use compared with native tissue vaginal prolapse repair. Urology 2012; 79(1): 12−4. 

Withagen MI, Milani AL, Boon J, Vervest HA, Vierhout ME. Trocar-guided mesh compared with conventional vaginal repair in recurrent prolapse: a randomized controlled trial. Obstet Gynecol 2011; 117(2 Pt 1): 242−50. 

Ek M, Altman D, Gunnarsson J, Falconer C, Tegerstedt G. Clinical efficacy of a trocar-guided mesh kit for repairing lateral defects. Int Urogynecol J 2013; 24(2): 249−54. 

Ignjatovic I, Stojkovic I, Basic D, Medojevic N, Potic M. Optimal primary minimally invasive treatment for patients with stress urinary incontinence and symptomatic pelvic organ prolapse: tension free slings with colporrhaphy, or Prolift with the tension free midurethral sling. Eur J Obstet Gynecol Reprod Biol 2010; 150(1): 97−101. 

37. Ignjatovic I, Stojkovic I, Stankovic J, Basic D, Potic M, Ignjatovic B. Simultaneous correction of anterior and apical vaginal prolapse with the modified placement of the transobturator-guided mesh (Anterior Prolift™) set. Urol Int 2011; 87(1): 14−8. 

38. Walters MD, Ridgeway BM. Surgical treatment of vaginal apex prolapse. Obstet Gynecol 2013; 121(2 Pt 1): 354−74. 

Ignjatovic I, Stosic D. Retrovesical haematoma after anterior Prolift® procedure for cystocele correction. Int Urogynecol J Pelvic Floor Dysfunct 2007; 18(12): 1495−7. 

El Haddad R, Svabik K, Masata J, Koleska T, Hubka P, Martan A. Women's quality of life and sexual function after transvaginal anterior repair with mesh insertion. Eur J Obstet Gynecol Reprod Biol 2013; 167(1): 110−3.

39. Ratner ES, Erekson EA, Minkin MJ, Foran-Tuller KA. Sexual satisfaction in the elderly female population: A special focus on women with gynecologic pathology. Maturitas 2011; 70(3): 210−5. 

40. Maher CM, Feiner B, Baessler K, Glazener CM. Surgical management of pelvic organ prolapse in women: the updated summary version Cochrane review. Int Urogynecol J 2011; 22(11): 1445−57.

41. FDA (2011) FDA safety communications: UPDATE on serious complications associated with the transvaginal placement of the surgical mesh for pelvic organ prolapse. 
Available from:
http://www.fda.gov/medical Devices/Safety/AlertandNotices/ucmucm262435htm [cited 2011 July 13].

Lee U, Wolff EM, Kobashi KC. Native tissue repairs in anterior vaginal prolapse surgery: examining definitions of surgical success in the mesh era. Curr Opin Urol 2012; 22(4): 265−70. 

Received on February 19, 2013.

Accepted on May 27, 2013. 

� EMBED Word.Picture.8  ���








Correspondence to: Ivan M. Ignjatović, Clinic of Urology, Clinical Center Niš, Bulevar Zorana Djindjica 46, 18 000 Niš, Serbia. 
Phone: +381 64 18 10 907. E-mail: ivanig@live.com
Petar Petrović, et al. Vojnosanit Pregl 2006; 63(1): 1–10.

[image: image2.wmf]

_1211955614.doc
[image: image1.png]






